Atomistic modelling of oxygen solute hardening in titanium alloys.
Tigany Zarrouk and Tony Paxton
Email: tigany.zarrouk@kcl.ac.uk
Department of Physics, King's College London, Strand, London WC2R 2LS, UK
Screw dislocations control plasticity in titanium.
Solute-hardening is not well understood on an atomistic scale.
Ab initio quantum mechanics is too computationally expensive.
Tight-binding approximation is quantum mechanical yet less expensive.
We have made a tight-binding model for titanium with which we can investigate atomistic mechanisms for oxygen solute-hardening.
Validation Tests
Tight-binding models need parameters.
Overlaps between atomic orbitals of atoms are parameters.
This titanium model is d-orbital only.
Ab initio Density Functional Theory (DFT) calculations and empirical quantities are fitted to.
Particle swarm algorithm used for fitting.
Validation achieved by comparison of:
Lattice wave dispersion (phonons).
Generalised stacking fault energy surfaces.
Dislocation core structure.
Dissolution/vacancy formation energies.
Quantity	Units	TB model	Literature
Evacancy formation	[eV]	1.01	1.27 [Exp. Hashimoto (1984)] / 1.95 [DFT Angsten (2013)]
ΔEsolution(tetra. - octa.)	[eV]	0.80	1.20 [DFT Kwasniak (2013)]
Phonons
 Experiment [2]
 Tight Binding
 G
 K
 M
 G
 A
Results of Fitting
Quantity	Units	TB model	Target
aα	[bohr]	5.52	5.57
c/a	ratio	1.571	1.587
C11	[GPa]	175.3	176.1
C33	[GPa]	195.5	190.5
C44	[GPa]	59.6	50.8
C12	[GPa]	70.2	86.9
C13	[GPa]	67.5	68.3
Quantity	Units	TB model	Target
aα	[bohr]	5.52	5.57
c/a	ratio	1.571	1.587
C11	[GPa]	175.3	176.1
C33	[GPa]	195.5	190.5
C44	[GPa]	59.6	50.8
C12	[GPa]	70.2	86.9
C13	[GPa]	67.5	68.3
Generalised Stacking Fault Energies
Gamma surfaces are plots of the excess energy of a faulted lattice, compared to an unfaulted one, with respect to fault vector.
Minima show areas where stable stacking faults occur.
These predict possible dislocation dissociations in the model.
DFT [3]
 Tight Binding
Method
Create dislocation in cell.
Put oxygen into different sites (octahedral) near core.
Relax cell to see how the core structure changes.
 Basal Plane
Predicted Splitting:
DFT: 1/3[1-210]  1/3[1-100] + 1/3[0-110]
TB: 1/3[1-210]  1/3[1-100] + 1/3[0-110]
 z
 x
 y
Periodicity along y
Dislocation Core Structure
Differential Displacement maps of screw dislocation core upon relaxation in tight-binding (TB) and Density Functional Theory (DFT / ab initio).
Arrows denote out-of-plane displacements.
An arrow joining two columns corresponds to displacement by a full Burger’s vector.
Position of elastic centre of dislocation core is marked by the red square.
Good agreement between model and DFT thus validating model.
 Prismatic Plane
Predicted Splitting:
DFT: 1/3[1-210]  1/6[1-210] + 1/6[1-210]
TB: 1/3[1-210]  (1/6[1-210] + 0.15[0001]) + (1/6[1-210] - 0.15[0001])
 Tight Binding
 Tight-binding
First order Pyramidal Plane.
Pseudopot. [4]
Predicted Splitting:
Pseudopotential: 1/3[2-1-13]  4/18[1-102] + 4/18[42-62] + 4/18[2-1-13]
        TB: 1/3[2-1-13]  4/18[1-102] + 4/18[42-62] + 4/18[2-1-13]
Applications:
Alloy design.
Stress-corrosion cracking.
Electrochemistry.
DFT [1]
References:
[1] Ghazisaeidi, (2012), Core structure of a screw dislocation in Ti from density functional theory and classical potentials
[2] Stassis, D. Arch, B. (1979), Lattice Dynamics of hcp Ti.
[3] Rodney, Ventelon (2016), Ab initio modelling of dislocation core properties in metals and semiconductors
[4] Ready (2019), Stacking faults and the γ-surface on {1-101} pyramidal planes in α-titanium.